Searching for Amorphous MgO Triple Junctions
2/08/16 Oliver Thomas

---
This week
- Investigate different quenching rates of the temperature to see if I can get a “frozen” structure.
- Simulate for a larger unit cell to see if multiple grains form.

---
12x12x2 Unit cell, 144 columns
MC stats:
- starting energy = -5925.6712 eV
- final energy = -5906.7988
- Disordered accepted MC moves = 792
- Disordered total moves = 5000
- Accepted MC moves = 412
- Total moves = 23800
- Ratio of accepted/Total = 1.73 %
- Immediate quenching from 500eV to 0.026eV

---
12x12x2 Unit cell, 144 columns

---
12x12x2 Unit cell, 144 columns
22000 to 28800 steps

---
New approach
- Implimented varying move distance, 1.0A to 1.5A for disorder phase. 0.5A for quenching. Should help system freezing into a higher energy state/not returning to lowest energy state.
- Haven't run yet due to the problems.

---
Problems
- Atom overlap is the biggest problem.
- Can't run in parallel, Infinite energy after moving a column with the set atom command when run on more than one processor when using mpirun -np x.

---
Atom overlap
- When columns get too close the potential massively decreases e.g. -10^-4 to -10^-6.
- Temporary fix by decreasing the temperature from 1000eV to 500eV.
- For the test cell case (perfect crystal structure) used the geometry optimised potential as the lowest value, if a move produced a lower energy than this base, reject the move.
- However this would only work for the test case as the lowest energy state is known, not valid for constrained case at grain boundaries.
- Didn't work anyway clusters of overlap atoms formed.

---
Atom overlap
- Tried setting the atoms to inlcude zero weighted bonds
- Compute bond/local dist - bond lengths were ~e20
- Tried setting the atoms to type sphere
- Compute pair/local dist
- Compute contact/atom – check if sphere is overlapping
- Can't find a way of using compute values in the program can only output them and use them for post processing – no good .